Editable Reconstructed Figures: Machining of Biomaterials

The three flowcharts below are reconstructed as native, editable Word objects. Every box is a table cell and every label is selectable, editable text - no diagram is embedded as an image.

Figure 1

Machining of Biomaterials

| ↓ | ↓ | ↓ |
| --- | --- | --- |

| Titanium Alloy Machining Ti-6Al-4V implants | Parametric Optimization Best Ra = 0.34 µm | Hybrid Manufacturing AM + CNC, EBM parts |
| --- | --- | --- |

↓

Outcome: Better Surface Quality, Reduced Tool Wear, Optimized Performance

Figure 1. Machining of biomaterials: pathways to improved surface quality and performance.

Figure 2

Computational Optimization and Performance Evaluation

| ↓ | ↓ | ↓ |
| --- | --- | --- |

| Multi-Objective Optimization Using GA, PSO and GRA • Optimizes MRR, roughness, tool wear together • Finds Pareto-optimal solutions | Genetic Algorithms (GA) • Based on natural selection • Selection, crossover, mutation • Optimizes turning parameters | Particle Swarm (PSO) • Inspired by bird flocking • Searches for best solution • Fast convergence, simple use |
| --- | --- | --- |

Figure 2. Computational optimization methods for machining parameter evaluation.

Figure 3

Industrial Case Studies on Patient-Specific Implants and Medical Device Manufacturing

| ↓ | ↓ |
| --- | --- |

| Case Study: Hip Prosthesis Manufacturing • CNC turning of hip prosthesis components using titanium alloys • Alloys studied: Ti-6Al-4V, Ti-6Al-7Nb, Ti-13Nb-13Zr • Minimum roughness Ra = 0.44 µm at feed rate 0.1 mm/rev for Ti-6Al-4V • Ti-13Nb-13Zr showed lower cutting forces at all feed rates • Surface quality affects osseointegration and implant life | Case Study: Additively Manufactured Femoral Cones • Post-processing of femoral cones made by electron beam melting (EBM) • ~30% reduction in cutting forces vs. wrought Ti-6Al-4V • 'Shell' effect of EBM specimens had no significant impact on cutting forces or roughness • Part orientation significantly affects machined surface quality |
| --- | --- |

↓

Optimized Machining Parameters → Improved Surface Quality and Precision → Better Osseointegration and Implant Life → Enhanced Production Efficiency

Figure 3. Industrial case studies linking optimized machining to implant performance.